| Title | Install mortar beds, self levellers, and screed compounds for tiled surfaces on site |
| --- | --- |
| Level | 4 | Credits | 12 |

| Purpose | People credited with this unit standard are able to: demonstrate knowledge of mortar beds, self levellers, and screed compounds, prepare and install mortar beds, self-levellers, and screed compounds for tiled surfaces on site, and complete work operations. |
| --- | --- |

| Classification | Construction Trades > Floor and Wall Tiling |
| --- | --- |

| Available grade | Achieved |
| --- | --- |

Guidance Information

1	Definitions

Specifications refers to documented instructions (oral, written, graphic) and may include any of the following: manufacturer’s specifications, recommendations or technical data sheets; material specifications; specifications from a specialist source such as an architect, designer, engineer or a supervisor; site or work specific requirements.

Surfaces refers to walls or floors of concrete, fibre cement, plaster board, timber flooring, tile, acoustic membrane, butyl rubber, rendered surface, cork tile, metal, glass, painted surface, or plastic.  Types of surface may include internal, external, wet, dry, new, existing, painted and unpainted.

Work site practice refers to the documented procedures specific to a work site which set out the standard and required practices of that work site.

2	For all on-site unit standards the practical assessment evidence must be provided in the context of commercial business construction operations, in the workplace, under normal workplace conditions.

3	Credit for this unit standard indicates compliance with industry practice.  Industry practice refers to the ability to work unsupervised, demonstrating knowledge and skills that reflect the productivity, uniformity, finish quality and material economies currently accepted within industry.

4	Typically, the laying of mortar beds, self-levellers, and screed compounds occurs in a variety of situations with variable time allowances and a number of different possible set-ups.  For assessment against this unit standard, evidence is required of at least two different installation situations which differ in terms of time allowances and set-ups.

5	Legislation and publications relevant to this unit standard include:

Health and Safety in Employment Act 1992 and Health and Safety in Employment Regulations 1995;

Building Act 2004;

Resource Management Act 1991;

AS 3958.1:2007, Ceramic tiles - Guide to the installation of ceramic tiles; available from http://infostore.saiglobal.com/store2/Details.aspx?ProductID=306963.

Outcomes and performance criteria

Outcome 1

Demonstrate knowledge of mortar beds, self levellers, and screed compounds.

Performance criteria

  - Mortar beds, self levellers, and screed compounds are described in terms of purpose and function.

  - Mortar beds, self levellers, and screed compounds are described in terms of substrates for which they are suitable in accordance with specifications.

  - Separating layers are described in terms of purpose, function, and relevance to types of mortar beds, self levellers, and screed compounds.

  - Mortar beds, self levellers, and screed compounds are described in terms of contents, mixing ratios, and mixing techniques.

  - Reinforcing and bonding coat requirements are described in relation to thickness of mortar beds, self levellers, and screed compounds.

  - Installation of mortar beds, self levellers, and screed compounds is described in accordance with job specifications.

Outcome 2

Prepare and install mortar beds, self levellers, and screed compounds for tiled surfaces on site.

Range	shower base;

one of – levels and falls, risers, treads.

Performance criteria

  - Surfaces to be tiled are identified and checked for compliance with specifications, and actions are taken in the event of non-compliance in accordance with work site practice.

  - Any work of other trades is identified and protected against damage from work operations.

  - Compounds are mixed in accordance with job specifications and work site practice.

Range	manually, mechanically.

  - Separating layer is applied in accordance with job specifications.

  - Bond application is compatible with surface and adhesives used in accordance with manufacturer’s specifications.

  - Bed is installed in accordance with job and manufacturer’s specifications.

Range	setting timelines, temperature ranges, application methods, finish.

Outcome 3

Complete work operations.

Performance criteria

3.1	All operations are safely completed; workplace, tools, plant and equipment are cleaned; and tools, plant and equipment are stored in accordance with work site practice.

| Replacement information | This unit standard replaced unit standard 22030 |
| --- | --- |

This unit standard is expiring.  Assessment against the standard must take place by the last date for assessment set out below.

Status information and last date for assessment for superseded versions

| Process | Version | Date | Last Date for Assessment |
| --- | --- | --- | --- |
| Registration | 1 | 18 February 2011 | 31 December 2024 |
| Review | 2 | 30 June 2022 | 31 December 2024 |

| Consent and Moderation Requirements (CMR) reference | 0048 |
| --- | --- |

This CMR can be accessed at http://www.nzqa.govt.nz/framework/search/index.do.